## Slide 1
National Institute of Advanced Industrial Science and Technology (AIST)
Spintronics Research Center
Tsukuba, Japan
In collaboration with:
S.P. Dash, Chalmers University of Technology, Göteborg, Sweden
J.C. Le Breton, FOM, Utrecht, The Netherlands
A.M. Deac, Helmholtz-Zentrum Dresden-Rossendorf, Dresden, Germany
B.C. Min, KIST, Seoul, Korea
S.C. Shin, KAIST, Daejeon and DGIST, Daegu, Korea
B.J. van Wees, University of Groningen, Groningen, The Netherlands
Ron Jansen
S. Sharma, A. Spiesser,
K. R. Jeon, S. Iba,
H. Saito, S. Yuasa.
Silicon spintronics

## Slide 2
IEEE Magnetics Society Home Page: www.ieeemagnetics.org
  3000 full members
  300 student members
The Society
  Conference organization (INTERMAG, MMM, TMRC, etc.)
  Student support for conferences
  Large conference discounts for members
  Graduate Student Summer Schools
  Local chapter activities
  Distinguished lecturers
IEEE Transactions on Magnetics
IEEE Magnetics Letters
Online applications for IEEE membership: www.ieee.org/join
  360,000 members
  IEEE student membership / IEEE full membership

## Slide 3
Spintronics
Thermoelectrics
Spin
Heat
Charge
Spin-caloritronics

## Slide 4
Issues in computing based on charge
Concerns about continuation of scaling down
Heat generated by electronic components limits performance
Computing is increasing fraction of world’s energy consumption
 Need for alternative, low power solutions

## Slide 5
Combining the best of both worlds
Ferromagnets
Non-volatile memory
Fast switching
High ordering temp.
Spin transport
Technology base (magnetic recording)
Semiconductors
Bandgap engineering - Carrier density & type -
Electrical gating -
Long spin lifetime -
Technology base - (electronics)
Semiconductor Spintronics a new technology based on spin

## Slide 6
Data processing
Semiconductors
Data storage
Ferromagnets
L2 cache(SRAM)
Main memory (DRAM)
Storage (HDD, SSD)
Logic
Register
L1 cache
L3 cache (SRAM)
Present state
Volatile
Non-volatile
Courtesy of K. Ando
Computer hierarchy & spin

## Slide 7
Data processing
Semiconductors
Data storage
Ferromagnets
L2 cache(SRAM)
Main memory (DRAM)
Storage (HDD, SSD)
Logic
Register
L1 cache
L3 cache (SRAM)
High-density STT-MRAM
Spin-FET, Spin Logic
Ultrahigh-density HDD MgO-MTJ read head
High-speed STT-MRAM
Present state
Volatile
Non-volatile
Semiconductor spintronics
Target
Metal-based spintronics
Courtesy of K. Ando
Computer hierarchy & spin

## Slide 8
Spin transistors
Spin diodes
Spin circuits and spin logic
Proposed spin-based device and systems

## Slide 9
Building blocks of silicon spintronics
Magnetic field
Electric field
Ferromagnetic tunnel contact
Ferromagnetic tunnel contact
Create spin
Detect spin
Manipulate spin
0  1

## Slide 10
Topics
Creating spin polarization in silicon by heat
Electrical creation/detection of spin polarization in Si
Combining electrical and thermal spin currents
&
Voltage tuning of thermal spin currents

## Slide 11
 =   
Transfer of spins by spin-polarized tunneling Creates spin accumulation

IT  IT
n  n
E
Creation of spin polarization in semiconductors by electrical injection from a ferromagnetic tunnel contact
Supply of spins by current
Spin relaxation in semiconductor


## Slide 12
Spin manipulation & detection
Precession of spins in transverse magnetic field (Hanle effect)

## Slide 13
S.P. Dash et al. Nature 462, 491 (2009)
Creating spin polarization in silicon at 300 K by electrical spin injection from a magnetic tunnel contact

## Slide 14
Electrical detection of spin polarization Resistance of tunnel contact is proportional to 
Tunnel spin polarization:
G  G
G  G
P =

## Slide 15
Silicon
MgO
Fe
0.5 - 2 nm
A. Spiesser et al.
Proc. SPIE 8461,
84610K (2012)
S. Sharma et al.
PRB 89, 075301 (2014)
Creation of spin polarization in silicon at 300 K Crystalline Fe / MgO tunnel contact
p-type Si (Boron, p = 5 x 1018 cm-3)

## Slide 16
MgO
Fe
Germanium
S. Iba et al., APEX 5, 053004 (2012)
Spintronics with p-type germanium at 300 K
Crystalline and Schottky free contacts

## Slide 17
Control experiment with Yb or Au nanolayer
Control device
Silicon / Al2O3 / Yb (2 nm) / Ni80Fe20
Standard
Silicon / Al2O3 / Ni80Fe20
Proof that signal is due to spin injection by tunneling
P = 0
P = 30%
Control device
Silicon / Al2O3 / Au (3 nm) / Ni80Fe20
Standard
Silicon / Al2O3 / Ni80Fe20
P = 0
P = 30%

## Slide 18
Spin lifetime and spin precession
near a tunnel interface
Electrical creation of spin polarization in silicon

## Slide 19
Spin lifetime in n-type silicon - Hanle vs. ESR
See reviews on Silicon Spintronics:
R. Jansen,
Nature Materials
11, 400 (2012)
R. Jansen et al.
Semicon. Sci.
Technol.
27, 083001 (2012)

## Slide 20
Extrinsic contributions to spin relaxation
spin precession in local magnetostatic fields
Inhomogeneous spin precession axis and frequency

## Slide 21
Spin relaxation near magnetic tunnel interface
role of ferromagnetic electrode
Ni80Fe20  0Msat = 0.9 T
Co  0Msat = 1.8 T
Fe  0Msat = 2.2 T
Injected spins feel
presence of the
ferromagnet !
 Apparent reduction
of spin lifetime
T = 300 K
p-Si = 4.8 1018 cm¯3 (B)

## Slide 22
Hanle effect and inverted Hanle effect
Spin precession in Bms
 reduced at Bexternal = 0
Bexternal in-plane, parallel to magnetization and injected spins, reduces precession
 recovery of 
Bexternal
Bms
S
Bms
S

## Slide 23
Hanle, inverted Hanle & anisotropy
p-type Si / Al2O3 / Fe
Anisotropy
Inverted Hanle effect:
spin precession modified by
inhomogeneous magnetic fields
(roughness, nuclear spins)
All characteristic
features of
spin precession and
spin accumulation

## Slide 24
Magnitude and scaling of the spin signal

## Slide 25
Spin current:
Spin resistance:
Resistivity spin-diffusion length

Js
Use Einstein relation:
rs =  Lsd
in m2
Magnitude of the spin accumulation
Expectation based on standard model for spin resistance

## Slide 26
Magnitude of the spin accumulation
disagreement between experiment and theory
See reviews on Silicon Spintronics:
R. Jansen,
Nature Materials
11, 400 (2012)
R. Jansen et al.
Semicon. Sci.
Technol.
27, 083001 (2012)

## Slide 27
Theory proposals to explain the disagreement
Localized states in the oxide barrier or at the oxide/semiconductor interface
First proposal by Tran et al.
PRL 102, 036601 (2009)
Recent extension by Song and Dery
PRL 113, 047205 (2014)
- Same as Tran’s model, but
- added Coulomb repulsion energy U
- spin-dependent blocking for eV >> kT
- Two-step tunneling
- spin accumulation in localized states
- Hanle spin precession
But, experiments ………..

## Slide 28
Magnitude and scaling of spin signal
S. Sharma et al.
PRB 89, 075301 (2014)
Theory:
V should be
proportional to J,
thus V / J is a
constant
Experiment:
spin-RA = V / J
scales with the
tunnel resistance
Not understood

## Slide 29
Magnitude of the spin signal for eV < kT
Data from S. Spiesser et al,
Jap. J. Appl. Phys. 52, 04CM01 (2013)
No spin signal reduction in the regime eV < kT,
 inconsistent with the theory of Song and Dery
Ge / GeO2 / Fe

## Slide 30
Control experiment with Ru metal instead of Si
Oxide but no semiconductor  no Hanle signal
Thus, signal does not originate from the tunnel oxide
S. Sharma et al. PRB 89, 075301 (2014)

## Slide 31
Can we create spin polarization in silicon
by heat, instead of charge current ?

## Slide 32
Thermal creation of spin polarization in Si
New phenomenon: Seebeck spin tunneling
Heat
flow
p.s. Zero charge
tunnel current !!

## Slide 33
Thermal spin current from ferromagnet to Si
Joule heating of Si
p-type Si / Al2O3 / Ni80Fe20, Tbase = 300 K, Si strip: 4000 x 800 x 3 m3

## Slide 34
Spin polarization induced by temperature difference only
No charge tunnel current
Thermal spin current from ferromagnet to Si
Observation of Seebeck spin tunneling
J.C. Le Breton et al.,
Nature 475, 82 (2011)

## Slide 35
Thermally-induced spin accumulation in Si
Scaling with Joule heating power
p-type Si / Al2O3 / Ni80Fe20 Tbase = 300 K
J.C. Le Breton et al., Nature 475, 82 (2011)

## Slide 36
Anisotropy of the Seebeck coefficient
J.C. Le Breton et al., Nature 475, 82 (2011), supplement
R. Jansen, Proc. SPIE 8813, 88130A (2013)
In-plane
Perpendicular
Anisotropy of S

## Slide 37
Origin of the thermal spin current

## Slide 38
Spin-polarized tunneling
G  G
Tunnel conductance is spin dependent
(1971)
Tunnel magnetoresistance
at 300 K (1995)
Electrical spin injection
(1999 - ……)

## Slide 39
Seebeck spin tunneling
Tunnel magneto-thermopower
(Walter et al. / Liebing et al. 2011)
Thermal spin injection
(Le Breton et al. 2011)
S  S
Seebeck coefficient of tunnel contact is spin dependent
(Le Breton et al. 2011)

## Slide 40
Electrical detection of Seebeck spin tunneling
VHanle
Thermally-induced
spin accumulation
Charge
thermopower

## Slide 41
Seebeck spin tunneling coefficient
Spin-dependent
Seebeck coefficient
electrical thermal
spin resistance
of semiconductor
Jansen, Deac et al.
PRB 85, 094401 (2012)

## Slide 42
Charge Seebeck effect
governed by energy derivative of charge conductivity
T1 T2
(E > EF)

(E < EF)

EF
E

## Slide 43
Seebeck spin tunneling (SST)
J.C. Le Breton et al., Nature 475, 82 (2011)

## Slide 44
Seebeck spin tunneling
Governed by energy derivative of tunnel spin polarization

## Slide 45
Sign of the thermal spin current

## Slide 46
Control of the sign of the spin polarization
by direction of heat flow
Reversing the heat flow  Opposite spin polarization
“negative spin polarization”
“positive spin polarization”
Jheat
Jheat

## Slide 47
Si heated
Sign reversal of thermal spin accumulation
FM heated

## Slide 48
Thermal + electrical spin currents
K.R. Jeon et al.
Nature Materials 13,
360 (2014)

## Slide 49
Simultaneous thermal & electrical driving force

## Slide 50
Thermal & electrical spin current together
Thermal
only
Thermal
+
electrical
spin
extraction
Thermal
+
electrical
spin
injection

## Slide 51
Voltage tuning of the thermal spin current

## Slide 52
Spin thermoelectrics away from Fermi energy
Conventional thermal spin
current near Fermi energy
Thermal spin current
at finite bias voltage
P
E

## Slide 53
Tuning of thermal spin current with voltage
Thermal spin current
at zero bias
Thermal spin current
with positive bias
K.R. Jeon et al.
Nature Materials 13,
360 (2014)

## Slide 54
Tunneling states
with a different
Voltage tuning of thermal spin current
n-type Si / MgO / Co70Fe30
Magnitude of thermal
spin current is tuned
by bias voltage
P
E

## Slide 55
For recent reviews of silicon spintronics, see
R. Jansen, Nature Materials 11, 400 (2012)
R. Jansen et al. Semicon. Sci. Technol. 27, 083001 (2012).
Electrical creation & detection of spin
polarization in Si using magnetic tunnel contacts
Thermal spin current into Si without a charge tunnel current, by Seebeck spin tunneling
Email: ron.jansen@aist.go.jp